# Technical Specification Sheet – ALgirba center

## A. Doors and Windows

| Item | Technical Description |
| --- | --- |
| Door 1.2×2.0 m | Galvanized steel sheet ≥1.2 mm thick, steel angle frame 40×40×3 mm, 3 heavy-duty hinges, standard lock, two coats of paint (anti-rust + finishing). |
| Two Doors 1×2 m | Galvanized steel sheet ≥1.2 mm thick, steel angle frame 40×40×3 mm, 3 hinges per door, medium-duty lock, two coats of paint. |
| Window 1×0.8 m | Steel angle frame 25×25×2.5 mm, glass or polycarbonate 4–6 mm thick, protection mesh, hinges and lock if required. |

## B. Reception Room (3×2 m)

| Item | Technical Description |
| --- | --- |
| External Zinc Cladding | Corrugated galvanized zinc sheets ≥0.4–0.5 mm thick, fixed on a galvanized steel frame. |
| Thermal Insulation | XPS boards, 50 mm thick, joints sealed with aluminum tape, 10–20 mm air gap between zinc and insulation. |
| Internal Lining | Moisture-resistant marine plywood, 12 mm thick, fixed with galvanized screws, two coats of moisture-resistant paint. |
| Fan Hook-up Point | with electrical box |
| Doors and Windows | As described above, including locks and hinges. |
| Painting | Two coats for metal and wood, all surfaces smooth and free from air bubbles. |

## C. Additional Works

| Item | Technical Description |
| --- | --- |
| Breaking Openings | Red brick with cement mortar (1:4), plaster 12 mm thick, surface leveling ±3 mm. |
| Floor screed motor (4×4 m) | Motor 1:3, slope .7% |

## D. Electrical work

| Item | Technical Description |
| --- | --- |
| Wiring | Single core 2.5mm (ALFANAR) IN PVC tube (TRUNKS) |
| Fan | sealing fan (orient ) |
| Switches & Sockets | Heavy-duty, white plastic or bakelite, rated 13A, 250V. Installation height: Switches at 1.4 m, sockets at 0.4 m above finished floor level |
| Lighting Fixtures | Energy-efficient LED luminaires, IP-65 for outdoor, IP-44 for indoor. Ceiling or wall-mounted |

## D. Quality Acceptance Criteria

Doors open and close smoothly; hinges stable; locks operate properly.

Uniform paint, no peeling after 7 days.

XPS insulation firmly fixed, no gaps, joints sealed.

Floor tiles level, even joints, no broken tiles.

Wall plaster level within ±3 mm tolerance.

Electrical work and extension are organized  and safe

- Eng: Asim Sedig Mohamed ALhassan Ali

- Signature